Sediment Strainers

1.0 SCOPE:

All requirements are for PVC  Sediment Strainers and accessories.

2.0 MATERIALS:

U-PVC – Conforming to ASTM D1784 Cell Classification 12454A

FKM – VitonR Fluorocarbon Rubber

EPDM – Ethylene Propylene Diene Terpolymer Rubber

3.0 VALVES:

Sediment Strainers shall be PVC body with EPDM or FKM seals.  Valves shall be true-union design and constructed of transparent PVC.  Standard screens shall be 20 mesh PVC.

3.1 Approved Manufacturer

Valves shall be provided by Asahi/America, Inc. of Malden, MA with no approved equals.  Manufacturer must be ISO-9001 certified.

3.2 Pressure vs. Temperature

Valves shall have a pressure rating of:

150 PSI sizes 1/2" – 2”

85 PSI sizes 3” & 4”

4.0 ACCESSORIES:

4.1 Optional Screen Materials and Mesh

Screens are offered in either:  PVC –  20 Mesh (Standard)         316 SS – 20 Mesh

30 Mesh			              40 Mesh

40 Mesh				 60 Mesh

4.2 Clean-Out Valve

Sediment Strainers shall accept the installation of a ¼” Labcock ball valve to be used as a  “Clean-Out” valve.  Clean-out valve must be factory installed by Asahi/America, Inc.

5.0 Certifications

PVC/EPDM and PVC/FKM models shall have NSF-61 Certification for use in drinking water applications.

6.0 INSTALLATION PROCEDURES:

All valve joints shall be prepared using either flanged, socket, or threaded connections.  The bolt diameters, torque values, and joining methods should be in accordance with the requirements put forth in the Sediment Strainer Operation & Maintenance manual.  All accessories should be installed in accordance with the manufacturers requirements as well as any facility requirements.